B4_lower_stock

Index to expected unit cell, sample is single

B4_below_weld

Expanded unit cell in the a and b directions, slight twinning.

Lowerstockredo

Sample is single indexs to expected unit cell

B4_belowweldr

Indexs to expected unit cell, single

B4_belowweldr2

Index to a different unit than expected, twinned sample, found expected unit cell through cell now. 1 above the weld, 2 below.

B4_weldarea

Refines to expected unit cell, sample is single

B4_weldarea2

Indexes to expected unit cell, sample is single

B4_crack feature

Index as expected, sample is single

B4_weldarea3

Indexes as expected, sample still single

B4_weldarea4

Indexes to expected unit cell, sample is single

B4_weldarea5

Sample indexes to expected unit cell, sample is single.