

Weld12

Clear section just below cloudy area

Fast scan collected at kappa=0 (perpendicular to X-ray beam)

Single and indexes with expected HR cell





Looks like c axis across fibre rather than along it – try point further down on fibre

Repositioned and fast scan on ground section

