Efficiently red-emitting dimethoxybenzothiadiazoles for organic doping-free devices enabling stable warm-white electroluminescence

Stepan Kutsiy,1 Lyudmyla Kanibolotska,2 Alexander Kanibolotsky,2,3 Mykhailo Shchetinin,1 Khrystyna Ivaniuk,1 Pavlo Stakhira,1 Asta Dabuliene,4 Dmytro Volyniuk,4* Joseph Cameron,2 Juozas V. Grazulevicius,4* Iryna Yaremchuk,1* Peter J. Skabara2*

1 Department of Electronic Engineering, Lviv Polytechnic National University, Sviatoho Yura sq. 1, Lviv 79013, Ukraine. E-mail: stepan.a.kutsii@lpnu.ua

2 School of Chemistry, University of Glasgow, Glasgow, G12 8QQ, United Kingdom

3 Institute of Physical-Organic Chemistry and Coal Chemistry, 02160 Kyiv, Ukraine

4 Department of Polymer Chemistry and Technology, Kaunas University of Technology, Barsausko 59, LT-51423, Kaunas, Lithuania. E-mails: dmytro.volyniuk@ktu.lt, juozas.grazulevicius@ktu.lt

| a | b |
| --- | --- |
| c |  |

Figure 2.	The cyclic voltammograms of (a) DiMeOBTTMS and (b) DiMeOBTH in 0.3 mM solution in CH2Cl2 with 0.1 M TBAPF6 as supporting electrolyte, glassy carbon disc as a working electrode, platinum wire as a counter electrode and silver wire as a quasi-reference electrode. The potential is referenced to the Fc/Fc+ redox couple. (c) The structure of the tetramethyl analogue of DiMeOBTTMS. The C3-Th–C2-Th–C4-BT–C3a-BT torsion angle is shown. The close contacts are shown by red (S···O) and blue (N···H) dashed lines.

| a | b |
| --- | --- |
| c | d |

Figure 3.	Absorption and PL spectra (a, b) and PL decay curves (c, d) of the dilute solutions of DiMeOBTTMS and DiMeOBTH in the various solvents. Absorption spectra are represented by dashed curves, while PL spectra are depicted by solid curves. Absorption and PL spectra of other solutions are provided in Figure S7.

| a | b |
| --- | --- |
| c | d |

Figure 4.	PL spectra (a, b) and PL decay curves (c, d) of host-based (Zeonex or CBP) and neat films of compounds DiMeOBTTMS and DiMeOBTH.

| a | b |
| --- | --- |

Figure 5.	Photoelectron emission spectra (a) and electric field dependences of hole mobilities (b) of vacuum-deposited layers of DiMeOBTTMS and DiMeOBTH. The inset shows TOF samples with the structure ITO/film/Al under UV excitation.

| a | b |
| --- | --- |
| c | d |

Figure 6.	EL spectra (a, b) at 10 V and corresponding CIE1931 colour diagram (c) of devices containing DiMeOBTTMS (a, c) and DiMeOBTH (b, c). The CIE1931 colour diagram contains CIE1931 colour coordinates of high-energy TADF emitters CBP:PO-T2T and DACT-II taken using their PL spectra. EL spectra (d) of device F at different voltages.

| a | b |
| --- | --- |
| c | d |

Figure 7.	Current density-brightness-voltage (a, b) and EQE-brightness (c, d) dependences of devices containing DiMeOBTTMS (a,c ) and DiMeOBTH (b, d).

| a | b |
| --- | --- |

Figure 8.	PL intensity as the 2D map (a) and the corresponding PL spectra (b) at different times after excitation of the DiMeOBTTMS/DACT-II film.