Supporting Information

Efficiently red-emitting dimethoxybenzothiadiazoles for organic doping-free devices enabling stable warm-white electroluminescence

Stepan Kutsiy,1 Lyudmyla Kanibolotska,2 Alexander Kanibolotsky,2,3 Mykhailo Shchetinin,1 Khrystyna Ivaniuk,1 Pavlo Stakhira,1 Asta Dabuliene,4 Dmytro Volyniuk,4* Joseph Cameron,2 Juozas V. Grazulevicius,4* Iryna Yaremchuk,1* Peter J. Skabara2*

1 Department of Electronic Engineering, Lviv Polytechnic National University, Sviatoho Yura sq. 1, Lviv 79013, Ukraine. E-mail stepan.a.kutsii@lpnu.ua

2 School of Chemistry, University of Glasgow, Glasgow, G12 8QQ, United Kingdom

3 Institute of Physical-Organic Chemistry and Coal Chemistry, 02160 Kyiv, Ukraine

4 Department of Polymer Chemistry and Technology, Kaunas University of Technology, Barsausko 59, LT-51423, Kaunas, Lithuania. E-mails: dmytro.volyniuk@ktu.lt, juozas.grazulevicius@ktu.lt

Figure S1.	1H NMR spectrum of 4,7-bis[5-(9,9-Dihexyl-7-(trimethylsilyl)-9H-fluoren-2-yl)-2-thienyl]-5,6-dimethoxy-2,1,3-benzothiadiazole (DiMeOBTTMS).

Figure S2.	13C NMR spectrum of 4,7-bis[5-(9,9-Dihexyl-7-(trimethylsilyl)-9H-fluoren-2-yl)-2-thienyl]-5,6-dimethoxy-2,1,3-benzothiadiazole (DiMeOBTTMS).

Figure S3.	1H NMR spectrum of 4,7-bis[5-(9,9-Dihexyl-9H-fluoren-2-yl)-2-thienyl]-5,6-dimethoxy-2,1,3-benzothiadiazole (DiMeOBTH).

Figure S4.	13C NMR spectrum of 4,7-bis[5-(9,9-Dihexyl-9H-fluoren-2-yl)-2-thienyl]-5,6-dimethoxy-2,1,3-benzothiadiazole (DiMeOBTH).

Figure S5.	Structure, HOMO and LUMO of 4,7-bis[5-(9,9-Dihexyl-7-(trimethylsilyl)-9H-fluoren-2-yl)-2-thienyl]-5,6-dimethoxy-2,1,3-benzothiadiazole (DiMeOBTTMS) (left) and 4,7-bis[5-(9,9-Dihexyl-9H-fluoren-2-yl)-2-thienyl]-5,6-dimethoxy-2,1,3-benzothiadiazole (DiMeOBTH) (right). Optimisations carried out in gas phase at PBE0/6-31G(d,p) level of theory.

Table S1.	Notable bond lengths and dihedral angles from structures calculated using DFT. PBE0/6-31G(d,p), gas phase.

|  | DiMeOBTTMS | DiMeOBTH | BTTMS | BTH |
| --- | --- | --- | --- | --- |
| S – O, Å | 2.70 | 2.71 | - | - |
| S – O, Å | 2.70 | 2.71 | - | - |
| C-H – N, Å | 2.23 | 2.24 | 2.32 | 2.31 |
| C-H – N, Å | 2.24 | 2.24 | 2.32 | 2.31 |
| S-C-C-C dihedral 1, ° | 7.6 | 8.3 | -6.1 | -4.8 |
| S-C-C-C dihedral 2, ° | 7.6 | 8.3 | -6.1 | -4.8 |

Table S2.	Summary of calculated energies from TDDFT (Tamm-Dancoff approximation). PBE0/6-31G(d,p), gas phase.

|  | HOMO, eV | LUMO, eV | HOMO-LUMO, eV | S1, eV | T1, eV | EST, eV | Orbital overlap S1 | Orbital overlap T1 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DiMeOBTTMS | -5.13 | -2.41 | 2.72 | 2.28 (543 nm) | 1.57 (791 nm) | 0.71 | 0.67 | 0.57 |
| DiMeOBTH | -5.12 | -2.41 | 2.71 | 2.28 (543 nm) | 1.56 (793 nm) | 0.72 | 0.67 | 0.57 |

a)

b)					c)

Figure S6.	TGA (a) and DSC (b, c) curves of compounds DiMeOBTTMS and DiMeOBTH.

a						b

c						d

Figure S7.	Absorption (a, b) and PL (a, b) spectra of the dilute solutions of DiMeOBTTMS (a, c) and DiMeOBTH (b, d) compounds in different solvents.

Figure S8.	Stokes shift as a function of orientation polarizability (Lippert–Mataga plots) of the different solutions of the compounds DiMeOBTTMS and DiMeOBTH. The Lippert–Mataga plots were plotted according to the formula  ∆ν=2Δf4πε0hca3μe-μg2+∆ν0, where ∆ν is the Stokes shift assuming no solvation effect, h is Planck’s constant, c is the velocity of light in vacuum, and ε0 is the permittivity of the free space, and a is the Onsager cavity radius, Δf is the orientational polarizability of the solvent. Calculated slopes associated with the change in the dipole moment of the compound in the ground (μg) and excited (μe) states.

Figure S9.	PL spectra (the left) and PL decay curves (the right) of Zeonex or CBP-containing films with different concentrations of DiMeOBTTMS and DiMeOBTH recorded under air or vacuum.

Figure S10.	Fitting of electric field dependences of hole mobilities of vacuum-deposited layers of DiMeOBTTMS, DiMeOBTH and DACT-II according to the Poole-Frenkel prediction µh=µ0×exp(βE1/2) [L. Pautmeier, R. Richert, H. Bässler, Poole-Frenkel behaviour of charge transport in organic solids with off-diagonal disorder studied by Monte Carlo simulation, Synthetic Metals 37 (1990).

Figure S11.	TOF signals for holes and electrons in vacuum-deposited films of DiMeOBTTMS, DiMeOBTH and DACT-II.

a)

b)

c)

Figure S12.	Thickness measurements of vacuum-deposited films of DiMeOBTTMS (a) DiMeOBTH (b) and DACT-II (c) using the profilometer Profilm 3D.

a)

b)

c)

Figure S13.	Equilibrium energy diagram of doping-free devices A and B (a), host-based devices C and D (b) and double EMLs-based devices E and F (c).

Figure S14.	EL spectra of device A-F at different voltages.

Figure 15.	PL decay curves recorded for DiMeOBTTMS/DACT-II-based EML during a constant time of 180 s at wavelengths from 450 to 750 nm with a step of 1 nm.